# Opis:

High quality 2K Clear for panel repair and overall resprays. Good filling properties, excellent gloss and flow in combination with very good polishability. It is extremely stable when applied on vertical surfaces and it can be overcoated within 24 h without intermediate sanding.

# Suitable Substrates:

- Hyflow basecoat

- Hydrobase basecoat

Mix 2:1 with any of the following hardeners:

- H077 slow

- H066 normal

- H055 fast

- H044 super fast Potlife: 5h at 20°C

5-10% Hymax Thinner

16-18s / DIN 4 mm / 20 oC

Compliant 1.3 – 1.5 mm (2 spray passes)

2.0 - 2.5 bar inlet pressure 2 = 50 – 60 micron

HVLP 1.3 – 1.5 mm (2 spray passes)

0.7 bar atomization pressure 2 = 50 – 60 micron

Wait 10 min before increasing temperature Bake 20 min at 60 oC panel temperature

# Flash Point:

Solids Content:

Specific Gravity:

Coverage:

SDS:

Short Wave 8 min.

The object should be maintained at greater than 60cm from source.

Wear suitable protection

25oC

52.1 % by weight

0.985 kg/cm3

8 - 9 m2/l at 50 micron dry film thickness (theoretical)

See the safety data sheet